CONFINEMENT AS A TOOL TO PROBE AMORPHOUS ORDER
GIACOMO GRADENIGO
In collaboration with:
C. Cammarota, G. Biroli
Kyoto, Japan, 19th July 2013

---
Does confinement enhances or depresses the tendency to form a glass ?
Confinement: reduction of the volume available to the liquid
- Jackson C L and McKenna G B, Chem. Mater. 8, 2128–37 (1996)
- C. Alba-Simionesco, et al, J. Phys. Condens. Matter 18 (2006) R15.
Fig: Glass transition temperature Tg, obtained from calorimetric measures, versus pore diameter “d” for toluene confined in nanopores. Non monotonic behaviour!
“Cut-off” effect
Competing effects
diameter of the pore
Interaction with boundaries
Slowing down of the system

---
Competing effects in simulations
“Cut-off” effect: smaller cavities are faster.
Boundary influence: smaller cavities are slower.
A. Cavagna, T. S. Grigera, and P. Verrocchio, J. Chem.Phys. 136, 204502 (2012)
L. Berthier and W. Kob, Physical Review E 85, 011102 (2012)
P. Scheidler, W. Kob, K. Binder, 2002 Europhys. Lett. 59 701
Local relaxation time varying the distance from the wall

---
Effect on confinement on the tendency to form a glass
Definition and behaviour of static length-scales which are defined via “gedanken” confinement experiments
Difference and similarities between “amorphous” and “random” boundary conditions in the confining cavity

---
Amorphous boundary conditions:
Point-to-set correlation length
 Exponential number of amorphous states at low temperature
Configurational entropy
Free energy gain for the nucleation of a new amorphous state in a glass-forming liquid
R
(Kirkpatrick,Thirumalai,Wolynes, Phys.Rev.A, 1989)
Probability of finding the cavity, after equilibration, in the same amorphous state of the frozen boundaries
(Biroli,Bouchaud, J.Chem.Phys, 2004)
Frozen particles
Free particles
Point-to-set length:
crossover from ergodic (large R) to non ergodic (small R) cavities

---
Point-to-set correlations length in simulations
Crossover to a glass state
Overlap at the center of the cavity: average correlation between configurations equilibrated under the influence of amorphous boundaries
A threshold value of the overlap can be conventionally fixed
Biroli, Bouchaud, Cavagna, Grigera, Verrocchio, Nature Physics, 2008
L. Berthier and W. Kob, PRE 85, 011102 (2012)
Hocky, Markland, Reichman, PRL, 2012

---
Analytic results in a Kac glass model:
The crossover is a transition
3d Kac model: fully connected p-spin model with effective interaction range g and space dependent overlap field q(x)
At small enough temperatures:
Cavity configurational entropy
Discontinuous overlap jump at the point-to-set:
glass formation in small cavities!
Franz, Montanari, J. Phys. A Math. Theor. 40, (2007)

---
Beyond the point-to-set length:
Removal of amorphous boundaries
AMORPHOUS BOUNDARY CONDITIONS
… experimentally a hard task !
Same chemical interaction between inner liquid and boundaries
TAKE FEATURLESS BOUNDARIES: JUST CONFINEMENT!
Confinement:
reduction of the volume available to the glass-former
(hard walls, boundaries of a different material,etc...)
1) Equilibrate a sample
2) Freeze all particles outside sphere R
3) Equilibrate only inside sphere R

---
Kac glass model with featureless boundaries
Average free energy cost to keep the configuration at b inside the cavity constrained to a configuration equilibrated at b' outside the cavity
CONFINEMENT
Two possible equilibrium values of overlap between configurations inside the cavity 1RSB scenario

---
Kac glass model with random boundaries: definition of the confinement length
Configurational Entropy
Solutions!
Confinement length
Transition to a glass state
By squeezing the volume available to the system the configurational entropy vanishes: glass state

---
Kac glass model with random boundaries: definition of the confinement length
Configurational Entropy
Solutions!
Confinement length
Simple Liquid
Activated dynamics
Glass

---
Kac glass model with random boundaries: definition of the confinement length
Configurational Entropy
Solutions!
Amorphous boundary conditions
Confinement length
Different behaviour of the overlap with random boundaries!
1) Smooth growth of the average overlap at the centre of the cavity
2) Bimodal distribution of the overlap ruled by parameter “m”, 1RSB phase
Random boundary conditions

---
Random vs Amorphous boundary conditions
Glass
Activated Dynamics
Simple Liquid
Random boundary conditions
1RSB Glass
Not favoured by boundaries
All amorphous states are equally disfavoured
?
Amorphous boundary conditions
RS Glass
Favoured by boundaries
A single amorphous state is favoured
stable
metastable
stable
metastable

---
Kac glass model with random boundaries: Phase diagram
.
For small values of the cavity radius we find a continuous transition to a trivially blocked state!
Confinement:
C. Cammarota, G. Gradenigo and G. Biroli, arXiv 1305.3538
Phase-diagram with randomly pinned particles:
 C. Cammarota, G. Biroli, J. Chem. Phys. 138, 12A547 (2013)

---
Conclusions
- Point-to-set length and confinement length behave in the same way.
- Pure geometric confinement induce amorphous order
- Glassy state induced by confinement is rather different than the glass induce by amorphous boundary conditions.
Confinement is more similar to cooling.
Perspectives
- Inclusion of finite range correction in the Kac model
- Behaviour of the confinement lenght in system with realistic interaction
- Experimental/numerical test of results in small cavities: bimodal distribution of overlap?
- Experimental/numerical study of the relaxation time under confinement?

---
Analytic results in a Kac glass model:
The crossover becomes a transition
Franz, Montanari, J. Phys. A Math. Theor. 40, (2007)
Kac model: fully connected p-spin model with effective interaction range g
Free energy difference between high and low overlap solutions
Confinement with amorphous boundary conditions:
increase of the glass transition temperature
Point-to-set

---
Kac glass model with random boundaries: Phase diagram
.
For small values of the cavity radius we find a continuous transition to a trivially blocked state!
Confinement: C. Cammarota, G. Gradenigo and G. Biroli, arXiv 1305.3538
Phase-diagram with pinned particles: C. Cammarota, G. Biroli, J. Chem. Phys. 138, 12A547 (2013)