## Slide 1: Discontinuous shear-thickening in Brownian suspensions
Department of Physics, Nagoya University
Takeshi Kawasaki
（Collaborator）
Université de Montpellier, CNRS, Ludovic Berthier
T. Kawasaki, A. Ikeda, and L. Berthier, EPL 107, 28009 (2014).
T. Kawasaki and L. Berthier, arXiv:1804.06800.
Rheology of disordered particles - suspensions, glassy and granular materials; part I
Notes: Thank you so much for giving me an opportunity to give a seminar today.

## Slide 2: Suspension rheology
cf: Oil in water emulsion (diameter = 20 μm)
The flow curves show non-monotonic bahaviour -- there are several flow regimes.
✓Suspension rheology → complicated flow behaviours.
Flow curve:
Y. Otsubo and R. K. Prud’homme, Rheol. Acta 33, 29 (1994)
Notes: In this study I will focus on the suspension rheology, which show very complicated behaviours.
To investigate the flow behaviours we measure the flow curves.
Flow curves is a relation between viscousity eta and shear rate gammadot.
This is the flow curves of oil in water emulsions as a function of packing fraction.
Here we see that especially in the middle density as shear rate is increased the viscosity shows non-monotonic behaviour.

## Slide 3: Elements of flow curve
Newtonian
Shear thickening
Shear thinning
Elements of flow curve
http://ja.wikipedia.org/wiki/%E7%B3%96%E8%9C%9C
E. Brown and H. M. Jaeger, Rep. Prog. Phys. 77, 046602 (2014).
Notes: Flow curves are composed of roughly speaking three elements, thickening, thinning , and Newtonian.
If the viscosity is constant as shear rate changed it is Newtonian – which is like a simple liquid behavior.
The viscosity decreasing with gammadot means shear thinning, which is very familiar in our daily life.
For instance, spreading butter, jam, syrup on a bread we experience shear thinning.
On the other hand, thickening is not so familiar. This picture is an example of thickening, one can walk on the fluid.
歩みを止めると沈む。。。

## Slide 4: Flow curves of suspensions
Y. Otsubo and R. K. Prud’homme, Rheol. Acta 33, 29 (1994)
Full range of the flow curves are deserved to be understood.
H. M. Laun, Angew. Makromol. Chem. 123, 335 (1984).
Notes: Until recently, full range of the flow curve had not understood well even in recently.

## Slide 5: Recent progress: physical origins of the two Newtonians
A. Ikeda, L. Berthier, and P. Sollich, Phys. Rev. Lett. 109, 018301 (2012)
✓ Numerical simulations on overdamped frictionless sheared Brownian particles.
✓ Time scale for thermal motions
✓ Time scale for dissipation
→ Glass transition
Characterized by thermal fluctuation
→ Jamming transition
Characterized by interaction energy
)
Notes: Recently by using very simple model, understanding of some of the rheological regimes has been obtained.

## Slide 6: Two yieldings
Green Kubo formula:
The intersection:
The intersection:
The intersection:

## Slide 7: Adding inertia to the simple model
T. Kawasaki, A. Ikeda, and L. Berthier, EPL 107, 28009 (2014).
Experiments
Our numerical simulations
✓ Adding inertia to Ikeda et al., PRL (2012)

## Slide 8: Discontinuous shear thickening by experiments
H. M. Laun, Angew. Makromol. Chem. 123, 335 (1984).
✓Latex dispersion (experiment)
Discontinuous shear thickening is not reproduced by our earlier model [T. K, A. Ikeda, and L. Berthier, EPL 107, 28009 (2014)].
Notes: Discontinuous shear thickening cannot be reproduced by just adding inertia.

## Slide 9: Discontinuous shear thickening by computer simulations
✓Recent observations (Numerical simulations)
R. Seto et al., PRL 111, 218301 (2013).
・inertia ×
・tangential friction ○
・contact repulsive force○
・electro static force○
・hydrodynamic lubrication force○
Shear rate
viscosity
M. Otsuki and H. Hayakawa, PRE 83, 051301 (2011).
・inertia○
・tangential friction○
・contact repulsive force○
stress
Shear rate
Granular model
Bagnold law
Yet, most experiments study soft colloidal particles subject to thermal fluctuations.
Non-Brownian colloidal model

## Slide 10: Purpose of the present study
inertia ×
Contact friction ○
Contact repulsion (softness) ○
Thermal fluctuation○
We propose minimal model for colloidal suspensions, which reproduces experiments for discontinuous shear thickening (DST).
-- We show that the model with following forces is enough to reproduce many of the experiments.
We intentionally neglect hydrodynamics, electrostatics, lubrication, and inertia, but can nevertheless achieve quantitative agreement with experimental findings.

## Slide 11: Note: Recent work by Mari et al.
The thickening is scaled with the Péclet number.
We have obtained different conclusions: if we change softness, the flow curve will not be scaled with Péclet number.
R. Mari, R. Seto, J. F. Morris, and M. M. Denn, PNAS 112, 15326 (2015).

## Slide 12: Numerical methods
✓Eq. of motions:
✓Binary mixtures:
＊ 50:50 bidisperse. Size ratio 1:1.4.
＊ Particle number N = 1000 (10000)
✓Tangential friction:
＊Distinct Element method（DEM）．
P. A. Cundall, O. D. L. Strack, Geotechnique 29 47-65 (1979).
＊Friction coefficient:
Molecular dynamics simulation
✓Control parameters:
＊ Dimension less temperature :
＊ Packing fraction:

## Slide 13: Density dependence of the flow curve with frictional Brownian particles

## Slide 14: Changing dimensionless temperature
Tangential friction with thermal fluctuation lead discontinuous thickening.
Dimensionless temperature:

## Slide 15: Scaling law
Shear thickening onsets for both of shear stress and shear rate are scaled by.

## Slide 16: Discussion
Where , ．
Onset stress is determined by the interplay between the instantaneous thermal fluctuation and frictional force.
(due to FDT)
Instantaneous thermal fluctuations
Friction is dominant
Friction is not dominant
Discontinuous thickening
Frictional force

## Slide 17: DST in Brownian suspensions
Sketch:

## Slide 18: Discontinuous shear thickening for different temperatures
R. Mari, R. Seto, J. F. Morris, and M. M. Denn, PNAS 112, 15326 (2015).
envelope

## Slide 19: Comparisons to experiments
is significant for classifying the materials:
[3] N. J. Wagner and J. F. Brady, Phys. Today 62, 27 (2009).
[4] B. J. Maranzano and N. J. Wagner, J. Chem. Phys. 114, 10514 (2001).
[8] N. Fernandez, et al., Phys. Rev. Lett. 111, 108301 (2014).
[9] B. M. Guy, M. Hermes, and W. C. K. Poon, Phys. Rev. Lett. 115, 088304 (2015).
Experimental data:
Notes: Here, we compare to the actual experimental values. According to the literatures we can obtain the shear thickening onset stress.
From this onset value we can obtain the dimensionless temperature. These are very close to what we use in our simulations.
Note that Mari’s estimated onset value 5kT/a^3 are very different from experimental ones.
In fact, this dimensionless temperatures is significant for classifying the materials.

## Slide 20: Experiments vs simulations
( )
( )
Scaled viscosity
Scaled shear rate
Experiment
Simulation
( )
The factor 10 we find suggests that the viscosity of the experimental suspensions is about 10 times larger than the corresponding one in the simulations.

## Slide 21: Hydrodynamic interaction is dominant in low density
R. Mari, R. Seto, J. F. Morris, and M. M. Denn, PNAS 112, 15326 (2015).

## Slide 22: Conclusion
Frictional Brownian suspensions show discontinuous shear thickening.
Interplay between the particle softness and thermal fluctuation affect the shear thickening onset.
Shear thickening onset stress are characterized by not scaled by .
Full range of flow curve is now completely understood.
T. Kawasaki and L. Berthier, submitted